Burl:

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Defect Number** | : | 0104 | | | | | | | | | | | | | | |
| **Defect Name** | : | Burl | | | | | | | | | | | | | | |
| **Defect Type** | : | Isolated Defects | | | | | | | | | | | | | | |
| **Fabric Type** | : | Denim Bottomweights - Piece Dyed | | | | | | | | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | |
| Burl — This is the result of a knot after burling.  Severity: Minor  Category: III | | | | | | | | | | | | | | | | |
| **Defect Number** | | | : | | | | | | | | | | | | | 0045 | | | | | | |
| **Defect Name** | | | : | | | | | | | | | | | | | Warp Burl | | | | | | |
| **Defect Type** | | | : | | | | | | | | | | | | | Warp lines, vertical lines | | | | | | |
| **Fabric Type** | | | : | | | | | | | | | | | | | Denim Bottomweights - Piece Dyed | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | | | | | | |
| Warp Burl — This is the result of a warp slub having been removed with a burling tool.  Severity: Major  Category: I | | | | | | | | | | | | | | | | | | | | | | |
| **Defect Number** | | | | : | | | | | | | | | | | 0058 | | | | | | | | |
| **Defect Name** | | | | : | | | | | | | | | | | Burl | | | | | | | | |
| **Defect Type** | | | | : | | | | | | | | | | | Weft lines, horizontal lines | | | | | | | | |
| **Fabric Type** | | | | : | | | | | | | | | | | Bottomweights - Plain Weave Derivatives | | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | | | | | | | |
| Burl — This is the result of a jerked-in piece of yarn having been removed by pulling it from the selvage. While no yarns ruptured, an open place is left in the fabric.  Severity: Major  Category: II | | | | | | | | | | | | | | | | | | | | | | | |
| **Defect Number** | | | | | : | | | | | | | | | 0095 | | | |
| **Defect Name** | | | | | : | | | | | | | | | Burl Mark | | | |
| **Defect Type** | | | | | : | | | | | | | | | Weft lines, horizontal lines | | | |
| **Fabric Type** | | | | | : | | | | | | | | | Bottomweights - Plain Weave Derivatives | | | |
| **Description** | | | | | | | | | | | | | | | | | |
| Burl Mark — This is the result of a slub or piece of wild filling having been removed with the use of a burling tool.  Severity: Major  Category: II | | | | | | | | | | | | | | | | | |
| **Defect Number** | | | | | | : | | | | | | | 0096 | | | | | | | | |
| **Defect Name** | | | | | | : | | | | | | | Burl Mark | | | | | | | | |
| **Defect Type** | | | | | | : | | | | | | | Weft lines, horizontal lines | | | | | | | | |
| **Fabric Type** | | | | | | : | | | | | | | Shirting and Dress Goods - Chambray | | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | | | | | |
| Burl Mark — This is the result of a slub or piece of wild filling having been removed with the use of a burling tool.  Severity: Major  Category: II | | | | | | | | | | | | | | | | | | | | | |
| **Defect Number** | | | | | | | : | | | | | 0099 | | | | | | |
| **Defect Name** | | | | | | | : | | | | | Burl | | | | | | |
| **Defect Type** | | | | | | | : | | | | | Weft lines, horizontal lines | | | | | | |
| **Fabric Type** | | | | | | | : | | | | | Shirting and Dress Goods - Chambray | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | | |
| Burl — This is the result of a piece of wild filling having been removed with a burling tool.  Severity: Major  Category: II | | | | | | | | | | | | | | | | | | |
| **Defect Number** | | | | | | | | : | | | 0106 | | | | | | | | | |
| **Defect Name** | | | | | | | | : | | | Hang Pick or Loopy Filling | | | | | | | | | |
| **Defect Type** | | | | | | | | : | | | Isolated Defects | | | | | | | | | |
| **Fabric Type** | | | | | | | | : | | | Denim Bottomweights - Indigo Dyed | | | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | | | | |
| Hang Pick or Loopy Filling — This defect is the result of the filling hanging on the knot which appears approximately one-half inch above the filling loops in the photograph. During weaving, the filling hangs on the knot for a split second until freed by the stroke of the reed.  Severity: Minor  Category: III | | | | | | | | | | | | | | | | | | | | |
| **Defect Number** | | | | | | | | | : | 0110 | | | | | | | | | |
| **Defect Name** | | | | | | | | | : | Warp Burl | | | | | | | | | |
| **Defect Type** | | | | | | | | | : | Warp lines, vertical lines | | | | | | | | | |
| **Fabric Type** | | | | | | | | | : | Bottomweights - Twill Derivatives | | | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | | | |
| Warp Burl — A distortion resulting from some superfluous material such as a thick slub, waste, or wild yarn being removed with a burling tool.  Severity: Minor  Category: I | | | | | | | | | | | | | | | | | | | |