Color fly:

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Defect Number** | | | | | : | 0135 | | |
| **Defect Name** | | | | | : | Color Fly | | |
| **Defect Type** | | | | | : | Isolated Defects | | |
| **Fabric Type** | | | | | : | Denim Bottomweights - Piece Dyed | | |
| **Description** | | | | | | | | |
| Color Fly — This is the result of small amounts of colored fiber being spun into yarn of another stock. This can happen in the reworking of waste or where different fibers or colors are running in close proximity without adequate precaution being taken to prevent contamination.  Severity: Minor  Category: III | | | | | | | | |
| **efect Number** | | : | | 0083 | | |
| **Defect Name** | | : | | Foreign Fiber | | |
| **Defect Type** | | : | | Warp lines, vertical lines | | |
| **Fabric Type** | | : | | Bottomweights - Sateen Derivatives | | |
| **Description** | | | | | | |
| Foreign Fiber — This is the result of a piece of polyester waste being spun into a cotton warp yarn.  Severity: Major  Category: I | | | | | | |
| **efect Number** | : | | 0134 | | | | |
| **Defect Name** | : | | Color Fly | | | | |
| **Defect Type** | : | | Warp lines, vertical lines | | | | |
| **Fabric Type** | : | | Denim Bottomweights - Piece Dyed | | | | |
| **Description** | | | | | | | |
| Color Fly — This is the result of small amounts of colored fiber being spun into yarn of another stock. This can happen in the reworking of waste or where different fibers or colors are running in close proximity without adequate precaution being taken to prevent contamination.  Severity: Minor  Category: I | | | | | | | |