Coarse end

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Defect Number** | | | | | | | | | | | | | | : | 0023 | | | | | | | |
| **Defect Name** | | | | | | | | | | | | | | : | Coarse End | | | | | | | |
| **Defect Type** | | | | | | | | | | | | | | : | Warp lines, vertical lines | | | | | | | |
| **Fabric Type** | | | | | | | | | | | | | | : | Denim Bottomweights - Piece Dyed | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | | | | | | |
| Coarse End — This end, being twice the size of the regular ends, is the unwanted result of two bobbins of roving running in spinning in what commonly is referred to as doubling.  Severity: Minor  Category: I | | | | | | | | | | | | | | | | | | | | | | |
| **Defect Number** | | | | | | | | | | | | : | 0024 | | | | | | | | |
| **Defect Name** | | | | | | | | | | | | : | Coarse End | | | | | | | | |
| **Defect Type** | | | | | | | | | | | | : | Warp lines, vertical lines | | | | | | | | |
| **Fabric Type** | | | | | | | | | | | | : | Shirting and Dress Goods - Plain Weave | | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | | | | | |
| Coarse End — This end, being twice the size of the regular ends, is the unwanted result of two bobbins of roving running in spinning in what commonly is referred to as doubling.  Severity: Major  Category: I | | | | | | | | | | | | | | | | | | | | | |
| **Defect Number** | | | | | | | | | : | | 0055 | | | | | | | |
| **Defect Name** | | | | | | | | | : | | Coarse Pick | | | | | | | |
| **Defect Type** | | | | | | | | | : | | Weft lines, horizontal lines | | | | | | | |
| **Fabric Type** | | | | | | | | | : | | Denim Bottomweights - Piece Dyed | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | | |
| Coarse Pick — Two coarse picks are inserted into consecutive sheds.  Severity: Major  Category: II | | | | | | | | | | | | | | | | | | |
| **Defect Number** | | | | | | | : | 0056 | | | | | | | | | |
| **Defect Name** | | | | | | | : | Coarse Pick | | | | | | | | | |
| **Defect Type** | | | | | | | : | Weft lines, horizontal lines | | | | | | | | | |
| **Fabric Type** | | | | | | | : | Denim Bottomweights - Piece Dyed | | | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | |
| Coarse Pick — A single coarse pick is inserted.  Severity: Major  Category: II | | | | | | | | | | | | | | | | | |
| **Defect Number** | | | | : | | 0060 | | | | | | | | | |
| **Defect Name** | | | | : | | Coarse Pick | | | | | | | | | |
| **Defect Type** | | | | : | | Weft lines, horizontal lines | | | | | | | | | |
| **Fabric Type** | | | | : | | Shirting and Dress Goods - Plain Weave | | | | | | | | | |
| **Description** | | | | | | | | | | | | | | | |
| Coarse Pick — Consists of three picks of coarse filling.  Severity: Major  Category: II | | | | | | | | | | | | | | | |
| **Defect Number** | : | | 0062 | | | | | | | | | | | | | |
| **Defect Name** | : | | Coarse Pick | | | | | | | | | | | | | |
| **Defect Type** | : | | Weft lines, horizontal lines | | | | | | | | | | | | | |
| **Fabric Type** | : | | Bottomweights - Twill Derivatives | | | | | | | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | |
| Coarse Pick — The filling yarn inserted is coarser than specified.  Severity: Major  Category: II | | | | | | | | | | | | | | | | |
| **Defect Number** | | : | | | 0090 | | | | | | | | | | | | | | |
| **Defect Name** | | : | | | Coarse End | | | | | | | | | | | | | | |
| **Defect Type** | | : | | | Warp lines, vertical lines | | | | | | | | | | | | | | |
| **Fabric Type** | | : | | | Bottomweights - Sateen Derivatives | | | | | | | | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | | | |
| Coarse End — This is a slightly coarse end that would not have been noticeable had it not been accentuated by sueding.  Severity: Minor  Category: I | | | | | | | | | | | | | | | | | | | |
| **Defect Number** | | | | | | | | | | : | 0172 | | | | | | | | | |
| **Defect Name** | | | | | | | | | | : | Coarse Yarn | | | | | | | | | |
| **Defect Type** | | | | | | | | | | : | Weft lines, horizontal lines | | | | | | | | | |
| **Fabric Type** | | | | | | | | | | : | Double Knit Fabrics | | | | | | | | | |
| **Description** | | | | | | | | | | | | | | | | | | | | |
| Coarse Yarn — This is the result of one feed of yarn being much coarser than normal for the fabric. The result is barré. .  Severity: Major  Category: II | | | | | | | | | | | | | | | | | | | | |