Color spot:

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Defect Number** | | | : | 0131 | |
| **Defect Name** | | | : | Color Spot | |
| **Defect Type** | | | : | Warp lines, vertical lines | |
| **Fabric Type** | | | : | Shirting and Dress Goods - Chambray | |
| **Description** | | | | | |
| Color Spot — This is the result of one beam of a slasher set being spotted with indigo. The spot is spread out according to the proportion of that beam to the total number of beams in the set. In this case, one of eight.  Severity: Major  Category: I | | | | | |
| **Defect Number** | : | 0149 | | |
| **Defect Name** | : | Indigo Dye Range Stop | | |
| **Defect Type** | : | Warp lines, vertical lines | | |
| **Fabric Type** | : | Denim Bottomweights - Indigo Dyed | | |
| **Description** | | | | |
| Indigo Dye Range Stop — This is the result of a machine stop on an indigo range. In this case, one end on the indigo range contains approximately one-eight of the total ends in the loom warp. This condition exists in a filling wise band of approximately fifteen inches.  Severity: Major  Category: I | | | | |