Double end:

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Defect Number** | | | | | | | | | : | 0022F | | | | |
| **Defect Name** | | | | | | | | | : | Double End | | | | |
| **Defect Type** | | | | | | | | | : | Warp lines, vertical lines | | | | |
| **Fabric Type** | | | | | | | | | : | Denim Bottomweights - Piece Dyed | | | | |
| **Description** | | | | | | | | | | | | | | |
| Double End — This defect is the result of an extra end being woven into the fabric. The extra end creates small flat distortions in the twill line.  Severity: Minor  Category: I | | | | | | | | | | | | | | |
| **Defect Number** | | | | | | : | | 0022B | | |
| **Defect Name** | | | | | | : | | Double End | | |
| **Defect Type** | | | | | | : | | Warp lines, vertical lines | | |
| **Fabric Type** | | | | | | : | | Denim Bottomweights - Piece Dyed | | |
| **Description** | | | | | | | | | | |
| Double End — This defect is the result of an extra end being woven into the fabric. The extra end creates small flat distortions in the twill line.  Severity: Minor  Category: I | | | | | | | | | | |
| **Defect Number** | | | : | | 0027 | | | | | | |
| **Defect Name** | | | : | | Double End | | | | | | |
| **Defect Type** | | | : | | Warp lines, vertical lines | | | | | | |
| **Fabric Type** | | | : | | Shirting and Dress Goods - Chambray | | | | | | |
| **Description** | | | | | | | | | | | |
| Double End — This defect is the result of an extra end being woven double with a regular end of the fabric.  Severity: Major  Category: I | | | | | | | | | | | |
| **Defect Number** | : | 0034 | | | | | | | | | | | |
| **Defect Name** | : | Double End | | | | | | | | | | | |
| **Defect Type** | : | Warp lines, vertical lines | | | | | | | | | | | |
| **Fabric Type** | : | Shirting and Dress Goods - Chambray | | | | | | | | | | | |
| **Description** | | | | | | | | | | | | | |
| Double End — This defect is the result of an extra end being woven double with a regular end of the fabric.  Severity: Major  Category: I | | | | | | | | | | | | | |
| **Defect Number** | | | | : | | | 0170 | | | | | |
| **Defect Name** | | | | : | | | Double End | | | | | |
| **Defect Type** | | | | : | | | Warp lines, vertical lines | | | | | |
| **Fabric Type** | | | | : | | | Warp Knit Fabrics | | | | | |
| **Description** | | | | | | | | | | | | |
| Double End — While this appears as a dark end, it actually is caused by two ends of a finer denier being knit together as one.  Severity: Major  Category: I | | | | | | | | | | | | |