Draw back:

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Defect Number** | | | : | 0087 | |
| **Defect Name** | | | : | Drawbacks | |
| **Defect Type** | | | : | Warp lines, vertical lines | |
| **Fabric Type** | | | : | Shirting and Dress Goods - Chambray | |
| **Description** | | | | | |
| Drawbacks — These are defects caused by excessive tension gradually applied by some abnormal restriction. When the restriction is removed, the excess slack is woven gradually into the fabric. Drawbacks may vary in length from inches to yards and often result in ruptured ends.  Severity: Major  Category: I | | | | | |
| **efect Number** | : | 0088 | | |
| **Defect Name** | : | Drawbacks | | |
| **Defect Type** | : | Warp lines, vertical lines | | |
| **Fabric Type** | : | Shirting and Dress Goods - Plain Weave | | |
| **Description** | | | | |
| Drawbacks — These are defects caused by excessive tension gradually applied by some abnormal restriction. When the restriction is removed, the excess slack is woven gradually into the fabric. Drawbacks may vary in length from inches to yards and often result in ruptured ends.  Severity: Major  Category: I | | | | |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Defect Number** | | | | | : | 0089 | | |
| **Defect Name** | | | | | : | Drawbacks | | |
| **Defect Type** | | | | | : | Warp lines, vertical lines | | |
| **Fabric Type** | | | | | : | Denim Bottomweights - Indigo Dyed | | |
| **Description** | | | | | | | | |
| Drawbacks — These are defects caused by excessive tension gradually applied by some abnormal restriction. When the restriction is removed, the excess slack is woven gradually into the fabric. Drawbacks may vary in length from inches to yards and often result in ruptured ends.  Severity: Major  Category: I | | | | | | | | |
| **Defect Number** | | : | | 0107 | | |
| **Defect Name** | | : | | Drawback (Small) | | |
| **Defect Type** | | : | | Warp lines, vertical lines | | |
| **Fabric Type** | | : | | Denim Bottomweights - Indigo Dyed | | |
| **Description** | | | | | | |
| Drawback (Small) — This defect is the result of a mat-up behind the harness that causes the ends to run taut and force the undyed filling to dominate the cover of the fabric.  Severity: Minor  Category: I | | | | | | |
| **Defect Number** | : | | 0108 | | | | |
| **Defect Name** | : | | Drawback (Small) | | | | |
| **Defect Type** | : | | Warp lines, vertical lines | | | | |
| **Fabric Type** | : | | Denim Bottomweights - Piece Dyed | | | | |
| **Description** | | | | | | | |
| Drawback (Small) — This is a similar defect but in a piece-dyed fabric. In both cases, the mat-up is removed before an end ruptures. There is always a corresponding slackness of ends when the restriction is removed.  Severity: Minor  Category: I | | | | | | | |