Hang thread

|  |  |  |
| --- | --- | --- |
| **Defect Number** | : | 0091 |
| **Defect Name** | : | Hang Thread |
| **Defect Type** | : | Warp lines, vertical lines |
| **Fabric Type** | : | Bottomweights - Twill Derivatives |
| **Description** | | |
| Hang Thread — This is the result of a weaver failing to clip the excess thread after repairing a broken end and the cloth inspector failing to remove it in the final inspection. The thread on the face of the fabric restricts the penetration of dye into the fabric beneath it resulting in a light streak.  Severity: Major  Category: I | | |

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Defect Number** | | | : | 0165 | |
| **Defect Name** | | | : | Dragging End | |
| **Defect Type** | | | : | Warp lines, vertical lines | |
| **Fabric Type** | | | : | Warp Knit Fabrics | |
| **Description** | | | | | |
| Dragging End — This is the result of an end being knit under erratic and excessive tension. This quite often is caused by ends being entangled and/or trapped on the warp beam.  Severity: Major  Category: I | | | | | |
| **Related Defects** | | | | | |
| **Defect Number** | : | 0166 | | |
| **Defect Name** | : | End Out and Straying End | | |
| **Defect Type** | : | Warp lines, vertical lines | | |
| **Fabric Type** | : | Warp Knit Fabrics | | |
| **Description** | | | | |
| End Out and Straying End — This is the result of a broken end straying over and being knit irregularly into another area of the fabric.  Severity: Major  Category: I | | | | |