Misdraw color:

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Defect Number** | | | | | : | 0167 | | |
| **Defect Name** | | | | | : | Misdraw (Color) | | |
| **Defect Type** | | | | | : | Warp lines, vertical lines | | |
| **Fabric Type** | | | | | : | Warp Knit Fabrics | | |
| **Description** | | | | | | | | |
| Misdraw (Color) — This is usually the result of an end being threaded or drawn into the wrong guide bar. It may also result from mixing yarn. In some instances, it can be traced to a creeling error in warping, causing an end to appear out of position on the warp beam.  Severity: Major  Category: I | | | | | | | | |
| **Defect Number** | | | : | 0168 | | |
| **Defect Name** | | | : | Misdraw (Color) | | |
| **Defect Type** | | | : | Warp lines, vertical lines | | |
| **Fabric Type** | | | : | Warp Knit Fabrics | | |
| **Description** | | | | | | |
| Misdraw (Color) — This is usually the result of an end being threaded or drawn into the wrong guide bar. It may also result from mixing yarn. In some instances, it can be traced to a creeling error in warping, causing an end to appear out of position on the warp beam.  Severity: Major  Category: I | | | | | | |
| **Defect Number** | : | 0169 | | | | | |
| **Defect Name** | : | Misdraw (Color) | | | | | |
| **Defect Type** | : | Warp lines, vertical lines | | | | | |
| **Fabric Type** | : | Warp Knit Fabrics | | | | | |
| **Description** | | | | | | | |
| Misdraw (Color) — This is usually the result of an end being threaded or drawn into the wrong guide bar. It may also result from mixing yarn. In some instances, it can be traced to a creeling error in warping, causing an end to appear out of position on the warp beam.  Severity: Major  Category: I | | | | | | | |