Misdraw

|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Defect Number** | | | | | | | : | 0013 | | | |
| **Defect Name** | | | | | | | : | Harness Misdraw | | | |
| **Defect Type** | | | | | | | : | Warp lines, vertical lines | | | |
| **Fabric Type** | | | | | | | : | Denim Bottomweights - Piece Dyed | | | |
| **Description** | | | | | | | | | | | |
| Harness Misdraw — This is the result of two ends being drawn wrong through the harness. Instead of the 1-2-3-4 draw, they are drawn 1-3-2-4. This distorts the weave and breaks the twill line.  Severity: Major  Category: I | | | | | | | | | | | |
| **Defect Number** | | | | | : | 0015 | | |
| **Defect Name** | | | | | : | Harness Misdraw | | |
| **Defect Type** | | | | | : | Warp lines, vertical lines | | |
| **Fabric Type** | | | | | : | Bottomweights - Twill Derivatives | | |
| **Description** | | | | | | | | |
| Harness Misdraw — This is the result of ends being drawn wrong through the harness. This takes place in a plain weave section of the fabric resulting in what is commonly called a "flat."  Severity: Major  Category: I | | | | | | | | |
| **Defect Number** | | | : | 0026 | | | | | |
| **Defect Name** | | | : | Flat or Harness Misdraw | | | | | |
| **Defect Type** | | | : | Warp lines, vertical lines | | | | | |
| **Fabric Type** | | | : | Shirting and Dress Goods - Plain Weave | | | | | |
| **Description** | | | | | | | | | |
| Flat or Harness Misdraw — This harness misdraw results in two ends weaving as one and opposing two other ends weaving as one. This is commonly referred to as a "flat."  Severity: Major  Category: I | | | | | | | | | |
| **efect Number** | : | 0032 | | | | | | | | |
| **Defect Name** | : | Flat or Harness Misdraw | | | | | | | | |
| **Defect Type** | : | Warp lines, vertical lines | | | | | | | | |
| **Fabric Type** | : | Shirting and Dress Goods - Chambray | | | | | | | | |
| **Description** | | | | | | | | | | |
| Flat or Harness Misdraw — This harness misdraw results in two ends weaving as one and opposing two other ends weaving as one. This is commonly referred to as a "flat."  Severity: Major  Category: I | | | | | | | | | | |