Mixed yarn:

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Defect Number** | | | | | | | | | : | 0145 | | | | |
| **Defect Name** | | | | | | | | | : | Mixed Yarn | | | | |
| **Defect Type** | | | | | | | | | : | Warp lines, vertical lines | | | | |
| **Fabric Type** | | | | | | | | | : | Shirting and Dress Goods - Chambray | | | | |
| **Description** | | | | | | | | | | | | | | |
| Mixed Yarn — This is one warp end of an all-cotton yarn running in a 50/50 cotton/polyester blend. In this fabric, only the cotton is dyed so that the all-cotton yarn shows dark.  Severity: Major  Category: I | | | | | | | | | | | | | | |
| **Defect Number** | | | | | | | : | 0052 | | |
| **Defect Name** | | | | | | | : | Mixed Filling | | |
| **Defect Type** | | | | | | | : | Weft lines, horizontal lines | | |
| **Fabric Type** | | | | | | | : | Shirting and Dress Goods - Oxford or Basket | | |
| **Description** | | | | | | | | | | |
| Mixed Filling — The nubby effect, which is a desired characteristic of this fabric, is lost or greatly reduced by the difference in the filling at the top of the photograph. This constitutes a defect.  Severity: Major  Category: II | | | | | | | | | | |
| **Defect Number** | | | : | | | 0053 | | | | | |
| **Defect Name** | | | : | | | Mixed Filling | | | | | |
| **Defect Type** | | | : | | | Weft lines, horizontal lines | | | | | |
| **Fabric Type** | | | : | | | Denim Bottomweights - Piece Dyed | | | | | |
| **Description** | | | | | | | | | | | |
| Mixed Filling (also Filling Band) — This defect is the result of a bobbin of lightweight filing; the twill line is subdued and the shade is affected. Since it is a mixed filling problem on this 3/1 left hand twill, the defect is more noticeable from the back.  Severity: Major  Category: II | | | | | | | | | | | |
| **Defect Number** | | : | | 0173 | | | | | | | | | |
| **Defect Name** | | : | | Missing Yarn | | | | | | | | | |
| **Defect Type** | | : | | Weft lines, horizontal lines | | | | | | | | | |
| **Fabric Type** | | : | | Single Knit Fabrics | | | | | | | | | |
| **Description** | | | | | | | | | | | | | |
| Missing Yarn — This is the result of a machine continuing to run with one yarn broken and/or missing. The result is barré. .  Severity: Major  Category: II | | | | | | | | | | | | | |
| **Defect Number** | : | | | | 0175 | | | | | | | |
| **Defect Name** | : | | | | Missing Yarn | | | | | | | |
| **Defect Type** | : | | | | Weft lines, horizontal lines | | | | | | | |
| **Fabric Type** | : | | | | Single Knit Fabrics | | | | | | | |
| **Description** | | | | | | | | | | | | |
| Missing Yarn — This is the result of a machine continuing to run with one yarn broken and/or missing. The result is barré. .  Severity: Major  Category: II | | | | | | | | | | | | |