Open read

|  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Defect Number** | : | 0018 | | | | | | | | |
| **Defect Name** | : | Open Reed | | | | | | | | |
| **Defect Type** | : | Warp lines, vertical lines | | | | | | | | |
| **Fabric Type** | : | Denim Bottomweights - Piece Dyed | | | | | | | | |
| **Description** | | | | | | | | | | |
| Open Reed — This is the result of a bent reed wire leaving a crack in the fabric.  Severity: Major  Category: I | | | | | | | | | | |
| **Defect Number** | | | : | | | | | | | 0020 | | | | |
| **Defect Name** | | | : | | | | | | | Open Reed | | | | |
| **Defect Type** | | | : | | | | | | | Warp lines, vertical lines | | | | |
| **Fabric Type** | | | : | | | | | | | Denim Bottomweights - Indigo Dyed | | | | |
| **Description** | | | | | | | | | | | | | | |
| Open Reed — This defect is the result of a bent reed wire holding the warp ends apart exposing the filling.  Severity: Major  Category: I | | | | | | | | | | | | | | |
| **Defect Number** | | | | : | | | | | 0030 | | | | |
| **Defect Name** | | | | : | | | | | Reed Misdraw | | | | |
| **Defect Type** | | | | : | | | | | Warp lines, vertical lines | | | | |
| **Fabric Type** | | | | : | | | | | Shirting and Dress Goods - Chambray | | | | |
| **Description** | | | | | | | | | | | | | |
| Reed Misdraw — This defect is caused by an end being misdrawn into a dent next to the one designated.  Severity: Minor  Category: I | | | | | | | | | | | | | |
| **efect Number** | | | | | : | | | 0031 | | | |
| **Defect Name** | | | | | : | | | Open Reed | | | |
| **Defect Type** | | | | | : | | | Warp lines, vertical lines | | | |
| **Fabric Type** | | | | | : | | | Shirting and Dress Goods - Chambray | | | |
| **Description** | | | | | | | | | | | |
| Open Reed — This defect is the result of a bent reed wire holding the warp ends apart exposing the filling.  Severity: Major  Category: I | | | | | | | | | | | |
| **Defect Number** | | | | | | : | 0122 | | | | | |
| **Defect Name** | | | | | | : | Reedy | | | | | |
| **Defect Type** | | | | | | : | Warp lines, vertical lines | | | | | |
| **Fabric Type** | | | | | | : | Bottomweights - Twill Derivatives | | | | | |
| **Description** | | | | | | | | | | | | |
| Reedy — This condition can be caused by the wrong reed, wrong reed-draw arrangement, wrong loom setting, or a combination of any or all three. The effect is open streaks following the pattern of the reed wires. This is also referred to as "poor cover."  Severity: Major  Category: I | | | | | | | | | | | | |