Slack end:

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **efect Number** | | | | : | | 0019 | | |
| **Defect Name** | | | | : | | Slack End | | |
| **Defect Type** | | | | : | | Warp lines, vertical lines | | |
| **Fabric Type** | | | | : | | Denim Bottomweights - Piece Dyed | | |
| **Description** | | | | | | | | |
| Slack End — This is the result of an end broken far back on the loom beam being woven into the cloth without tension. This tends to pucker the yarn as it is woven.  Severity: Major  Category: I | | | | | | | | |
| **Defect Number** | | | : | | 0021 | |
| **Defect Name** | | | : | | Slack End | |
| **Defect Type** | | | : | | Warp lines, vertical lines | |
| **Fabric Type** | | | : | | Denim Bottomweights - Indigo Dyed | |
| **Description** | | | | | | |
| Slack End — This is the result of an end broken far back on the loom being woven into the cloth without tension. This tends to pucker the yarn as it is woven.  Severity: Major  Category: I | | | | | | |
| **Defect Number** | : | 0129 | | | | | |
| **Defect Name** | : | Slack Ends | | | | | |
| **Defect Type** | : | Warp lines, vertical lines | | | | | |
| **Fabric Type** | : | Denim Bottomweights - Piece Dyed | | | | | |
| **Description** | | | | | | | |
| Slack Ends — This shows the effect of a warp running out on a loom, resulting in a large number of ends weaving slack.  Severity: Major  Category: I | | | | | | | |