Soiled end:

|  |  |  |
| --- | --- | --- |
| **Defect Number** | : | 0084 |
| **Defect Name** | : | Soiled End |
| **Defect Type** | : | Warp lines, vertical lines |
| **Fabric Type** | : | Bottomweights - Twill Derivatives |
| **Description** | | |
| Soiled End — This end apparently had grease spun into it during the spinning operation.  Severity: Major  Category: I | | |

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Defect Number** | | | : | 0040 | |
| **Defect Name** | | | : | Soiled Filling | |
| **Defect Type** | | | : | Weft lines, horizontal lines | |
| **Fabric Type** | | | : | Shirting and Dress Goods - Chambray | |
| **Description** | | | | | |
| Soiled Filling — This description best suits the illustrated defect; however, this is package dyed filling and what appears as oily slubs actually is dye scum or crystallized dyestuff from the outside of the dye package. On a Sulzer loom, which feeds pick and pick from four dye packages simultaneously, this can continue as a general condition for a number of yards.  Severity: Major  Category: II | | | | | |
| **efect Number** | : | 0041 | | |
| **Defect Name** | : | Soiled Filling | | |
| **Defect Type** | : | Weft lines, horizontal lines | | |
| **Fabric Type** | : | Shirting and Dress Goods - Plain Weave | | |
| **Description** | | | | |
| Soiled Filling — This defect is the result of a drop of dirty oil on a bobbin of filling.  Severity: Major  Category: II | | | | |